Note S7 | Correlating LiF/HCl etching chemistry with the real-space/reciprocal-space lattice signatures of Ti3C2Tx MXene

Figure 8 integrates the chemical pathway of Ti₃C₂Tₓ formation with a solid-state, lattice-level validation by HRTEM and FFT. In the LiF/6 M HCl route, LiF dissolves in concentrated HCl to generate HF in situ (LiF + HCl → HF + LiCl), providing a controlled fluoride activity that selectively extracts Al from Ti3AlC2 while avoiding the excessive, instantaneous attack often associated with direct HF handling (Fig. 8a). Conditioning the MAX powder (drying and deagglomeration) reduces local packing density and promotes uniform wetting; together with portion wise MAX addition under vigorous stirring, these steps suppress foaming and temperature gradients and thereby minimize spatial heterogeneity in etch depth (Fig. 8a). The extended etching step (50 °C, 30 h) removes the Al layers and simultaneously establishes the characteristic surface terminations Tx = –F, –OH, and =O through reactions with fluoride and water in the acidic medium (Fig. 8b). From a crystallographic standpoint, this transformation preserves the 2D Ti–C backbone while converting the parent MAX into a terminated MXene with modified interlayer chemistry and enhanced propensity for solvation/rehydration. The post-etch separation and washing sequence is not merely a “cleanup” operation but a key determinant of microstructure. Centrifugation and repeated washing to pH 5–6 remove residual acid and soluble byproducts (Al³⁺ species, LiCl, excess fluorides), reducing uncontrolled ionic screening and mitigating continued surface attack (Fig. 8b). At the same time, progressive neutralization and termination equilibration change the interfacial energy landscape of the flakes, which promotes partial restacking/overlap during handling and drying via capillary forces and electrostatic collapse. This mesoscale consequence is directly visible in the HRTEM.

Figure 8c shows a high-resolution TEM image of MXene acquired at 200 kV (OneView; 1MX). The micrograph exhibits extended, electron-transparent domains with locally varying contrast and multiple lattice-fringe orientations. This combination is characteristic of few-layer nanosheets with partial restacking: crystalline in-plane order is retained within each flake, whereas overlap regions introduce rotational misalignment and weakly strained boundaries, which manifest as fringe bending and changes in local fringe direction rather than amorphous contrast.

To quantify the crystalline periodicity, three representative lattice-fringe-rich regions of interest (ROIs) were selected from the interior of the field of view (avoiding the scale-bar overlay and obvious thickness/contamination gradients), as shown in Fig. 8d-f. Each ROI was selected with a Hann window and analyzed using a 2D fast Fourier transform (FFT). Discrete maxima away from the central beam were consistently observed, confirming that the fringes originate from coherent lattice periodicity rather than imaging noise or random texture (Fig. 8g-i). Spatial calibration was performed directly from the scale bar embedded in the micrograph (10 nm). Using the measured bar length, the pixel size is Δx≈0.01253 nm px-1 (a conservative estimate based on the bar extent; the uncertainty associated with the bar outline corresponds to a few-percent systematic variation in Δx, and is propagated qualitatively below).

The dominant periodicity for each ROI was extracted from the strongest non-central FFT peak using d=(N× Δx)r, where N is the ROI size (512 px) and r is the radial distance of the FFT peak from the reciprocal-space origin (in pixels). The resulting spacings are 0.3073 nm (ROI-1), 0.3001 nm (ROI-2), and 0.2938 nm (ROI-3), yielding an average d=0.300±0.007nm (mean ± s.d., n=3). The narrow dispersion indicates robust in-plane order across different crystallites, while the residual spread is consistent with local strain/thickness variation and stacking disorder at flake overlap boundaries.

Indexing was performed within the common hexagonal basal-plane description used for many MXenes. The observed fringes are predominantly in-plane (no clear 00l periodicity is resolved in these ROIs), therefore l=0 and the measured periodicity is most consistently assigned to the {1010} family in Miller–Bravais notation (equivalently {100} in three-index notation), which often dominates for basal-plane ordering in layered hexagonal systems. Using d{1010}=32a, the in-plane lattice constant from the three ROIs are a=0.3469±0.0078 nm (mean ± s.d., n=3). Considering the small systematic uncertainty in Δx introduced by the scale-bar outline, a is best reported as a≈0.35 nm (few-percent uncertainty). Importantly, the present HRTEM dataset constrains in-plane ordering; extraction of the out-of-plane lattice parameter ccc (or interlayer gallery height) requires either clear 00l fringes in cross-sectional views or complementary low-angle diffraction (e.g., XRD/SAXS) where basal reflections are unambiguously resolved.