Figure 8 | LiF/HCl synthesis workflow and lattice-resolved TEM validation of Ti3C2Tx MXene. (a) Preparation of the LiF/6 M HCl etchant (30 °C, 500 rpm, 1 h) and MAX conditioning/portion wise Ti3AlC2 addition to ensure homogeneous wetting and reproducible etching. (b) Selective Al removal at 50 °C (500 rpm, 30 h), followed by separation and repeated washing/centrifugation to pH 5–6 to remove dissolved byproducts and residual acidity/fluorides while stabilizing surface terminations (Tx = –F/–OH/=O). (c) Representative HRTEM image (scale bar, 10 nm) revealing a mosaic of rotated crystalline domains consistent with few-layer flakes and partial restacking. (d)–(f) Lattice-fringe ROIs (scale bars, 2 nm). (g)–(i) Corresponding FFT patterns showing discrete reciprocal-space maxima. Dominant fringe spacings are 0.307, 0.300, and 0.294 nm (ROIs 1–3), yielding 0.300 ± 0.007 nm and an in-plane lattice constant a = 0.347 ± 0.008 nm (indexed to {1010}/{100}).